## Slide 1: SIS Detectors & Dielectric Stack Optical Diplexers
BREAD Collaboration Workshop
Edward Tong & Keara Carter
January 14th, 2026

## Slide 2
Some Basic Facts About SIS Detector/Mixer
wSMA 3-junction mixer
GHz
Cross-section view of an Nb/Al-AlOx/Nb junction
~150 nm
TypicallySiO2
SIS=Superconductor-Insulator-Superconductor Junction.
Most popular low noise heterodyne detector for 85 -1000 GHz
Quantum noise limited. Sensitivity: (24 K at 250 GHz)
Lowest noise operation: Double-side-band (DSB) mode.
Operation at 4 K or below. Only slight advantage at lower temperature.
Requires magnetic field to operate. Below 250 GHz, use of permanent magnet is OK.
May need to be shielded from strong external B-field.
Very mature technology.
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 3
Source: www.almaobservatory.org
A. R. Kerr, S. . -K. Pan and W. G. Lyons, "The genesis of SIS mixers - the legacy of John Tucker in radio astronomy," 2015 IEEE MTT-S International Microwave Symposium, Phoenix, AZ, USA, 2015, pp. 1-4, doi: 10.1109/MWSYM.2015.7166809.
ALMA – Atacama Large Millimeter Array
Highest concentration of deployed SIS mixers.
Over 1000 mixers are in active service on the 64 telescopes.
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 4
Introduction to the Submillimeter Array (SMA)
Mauna Kea
Hilo
Honolulu
SMA partnership:
Center for Astrophysics (CfA)
Academia Sinica, Taiwan
University of Hawaii
  World’s first imaging submm interferometer.
  Dedicated 2003.
  8x 6-meter dishes
  Dual band observation setup: currently operating in 230 and 345 GHz bands.
  Full polarimetric capabilities
  Supports hands-on instrument training.
  Platform for testing future submm instrumentation.
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 5
Incident Beam
 | Rx-A | Rx-B
Target LO Freq | 210 – 270 GHz | 280-360 GHz
Current LO Freq | 220 – 275 GHz | 324 – 357 GHz
IF subsystem | SAO-isolator + LNF-LNC6_20 LNA | 
Achieved IF | 4-15 GHz | 4-18 GHz
SIS B-field | Permanent Magnet | Electro-magnet
wSMA Receiver Cartridges
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 6
Isolator & Cryo Low Noise Amplifier (LNA)
LNF-LNC6_20D
4 K performance
Use of a ferrite isolator between the SIS mixer and LNA is important to get wide instantaneous BW (IF).
We developed a wideband ”edge-mode isolator” in our lab.
Zeng, Tong and Paine, “A Low-Insertion Loss Cryogenic Edge-Mode Isolator with 18 GHz Bandwidth,” IEEE Journal of Microwaves, Oct. 2023.
Pairing the edge-mode isolator with an appropriate LNA produces flat noise response between 4 and 19 GHz.

## Slide 7
Forward wave
Reverse wave
IN
OUT
OUT
IN
Credit: Lingzhen Zeng
Edge Mode Isolator: Electric Field Simulations
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 8
SIS Mixer for Black Hole Explorer Mission
Test Team
30 K ~ 2hv/k
SEM image
Chip Design: CfA
Fab: NAOJ Japan
Freq: 228 – 320 GHz
DSB mixer for space.
Initial test in Cambridge Dec. 2025.

## Slide 9
Record Noise Temperature
BPF
P
SIS Mixer
LO
Y-Factor Meas.
External LN2 Load 78.5 K
Internal cold Load 40 K
LO 345 GHz
Y = 3.04
Y = 5.08
Y | Tn [K] | 
3.04 | 29 | 1.75
5.08 | 23 | 1.4
Y | Tn [K] | 
3.04 | 29 | 1.75
5.08 | 23 | 1.4
SIS noise approaches quantum limit.
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 10
Sensitivity of SIS Mixer: Is it Good Enough for Axion Search?
SIS Rx
FPGA Spectrometer
15 GHz
Bif
DSB
Tn=30 K
Bchannel 1 MHz wide
Radiometer Equation
=1 sec
Min. detectable power
SIS Receiver offers very competitive sensitivity for a mature technology.
It would also pinpoint the energy of detected photon
Sweet spot for SIS receiver: 150 – 400 GHz
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026

## Slide 11
Next Trend: Simultaneous Multi-Band Receiver Set
86, 230 + 345 GHz Tri band
We have developed a dielectric stack optical diplexer.
BREAD Collaboration Workshop
Harvard University. Jan. 14, 2026
All Require Optical Multiplexing
80-106 GHz + 240-320 GHz Dual band
230 + 345 GHz Dual band
ngEHT

## Slide 12
Multi-Band Receiver System

## Slide 13
Tri-Band Receiver System

## Slide 14
Tri-Band Receiver System

## Slide 15
Tri-Band Receiver System
Diplexer #1:
Reflect 86-115 GHz
Transmit 230-345 GHz
Room temperature

## Slide 16
Tri-Band Receiver System
Diplexer #1:
Diplexer #2:
Reflect 345 GHz
Transmit 230 GHz
Cryogenic operation: 50K
Diplexer
Reflect 86-115 GHz
Transmit 230-345 GHz
Room temperature

## Slide 17
Our Diplexer:
Incoming Beam
Reflected Beam
Transmitted Beam
Rx-A
Rx-B
Telescope
angle of incidence
thickness of dielectric layer
Stack of dielectric materials
Diplexer
Diplexer

## Slide 18
Diplexer
Reflect 86-115 GHz
Transmit 230-345 GHz
Room temperature operation
Diplexer #1
25 layers
2.5mm thick stack

## Slide 19
Diplexer
Diplexer #2
3.34mm thick stack
Reflect 345 GHz
Transmit 230 GHz
Cryogenic operation: 50K

## Slide 20
Performance
Quasi-Optical Vector Network Analyzer (QO-VNA)

## Slide 21
Performance
Quasi-Optical Vector Network Analyzer (QO-VNA)
Reflect 86-115 GHz
Transmit 230-345 GHz
Room temperature operation
Diplexer #1

## Slide 22
Performance
Quasi-Optical Vector Network Analyzer (QO-VNA)
Reflect 345 GHz
Transmit 230 GHz
Cryogenic operation: 50K
Diplexer #2

## Slide 23
Performance
Y-Factor Measurements: Loss

## Slide 24
Performance
Y-Factor Measurements: Loss
Frequency (GHz) | Polarization | Measured Loss (%)
221 | Vertical (V) | 3.0
 | Horizontal (H) | 2.8
345 | Hpol | 1.3
Diplexer #1
Reflect 86-115 GHz
Transmit 230-345 GHz
Diplexer #2
Reflect 345 GHz
Transmit 230 GHz
Frequency (GHz) | Polarization | Measured Loss (%)
228 | V | 3.4
 | H | 1.6
240 | V | 1.1
 | H | 1.2
348 | V | 1.1

## Slide 25
Next Steps
Chart: 
Selector wheel positions:
Open port
Plane Mirror
Wire Grid
Diplexer (upcoming!)
Installation of diplexer #2 into test cryostat
Validation of performance and robustness at cryogenic temperatures

## Slide 26
Next Steps
Chart: 
Installation of diplexer #2 into test cryostat
Validation of performance and robustness at cryogenic temperatures
Installation of diplexer #2 into all wSMA cryostats in Hawaii

## Slide 27
Next Steps
Preliminary diplexer data modeling technique
(Donovan Flagg, summer 2025 ngEHT Intern)
QO-VNA Data

## Slide 28
Next Steps
Preliminary diplexer data modeling technique
(Donovan Flagg, summer 2025 ngEHT Intern)
Design dielectric multilayer stacks by specifying a target transmission response and solving for:
  required refractive indices
  layer thicknesses
  number of layers

## Slide 29
keara.carter@cfa.harvard.edu
etong@cfa.harvard.edu
Thank you for your time!
BREAD Collaboration Workshop
Edward Tong & Keara Carter
January 14th, 2026